Unipol 1210 Heavy Duty ( 12") Precision Grinding / Polishing Machine with Complete Accessories

UNIPOL- 1210 grinding / polishing machine is equipped with 12" lapping plate and can be used as a standard manual grinder, or lapping / polishing machine for both of flat sample and metallographic samples.  It is the most cost effective solution for material research lab to prepare metallographic samples

Features:

- Heavy duty steel case with beautiful painting surface

- Perfect for material Research and R&D laboratories to prepare metallurgical sample and failure analysis

- 12" dia lapping plate ( PVC wheel ) allows you to attach sand papers / polishing pads

- Power:                                    120V or 240 V  auto switching power supply, worldwide support

- Motor:                                     300 W high torque DC motor with one year warranty

- Variable speed:                      from 0 - 600 RPM with digital display

- Emergency Stop                     for immediate stop

- Dimension:                             560  L x 345 W  X 325 H (mm)

- Net weight:                        42 Kg

- Dimension of shipment:        36" x 30" x 22"

- Weight of shipment:               140 Lbs

- Complete accessories included for immediate using, including:  ( > $300 value, click underlined to order extra)

  - Two 12" dia lapping plate ( PVC wheel ) pre-installed with magnetic pad to allow you attaching sand papers / polishing pads

  - Two 12" PSA Diamond Lapping plates with 600 mesh and 800 mesh separately

  - Two 12" PSA black polishing pads for final polishing

  - One 10g  0.5 micron diamond paste for faster polishing

_____________________________________________________

MTI Corporation

860 South 19th Street, Richmond, CA 94804, USA

tel: 510-525-3070  fax: 510-525-4705   Email: sales@mtixtl.com  website: www.mtixtl.com