Certificate of Analysis

Aluminum (Al)

99+% (metal basis, O < 10%), APS 18 nm

Stock #: 0136JY

| Components | Contents (%) |
| --- | --- |
| Ca | 0.47 |
| Cu | 0.008 |
| Mn | 0.002 |

Analytical Technique: inductively coupled plasma