Certificate of Analysis

Aluminum oxide (Gamma), 30 nm, ( 99.99%

| Components | Contents (ppm) |
| --- | --- |
| Ca | 1.6 |
| Co | 0.8 |
| Fe | 0.2 |
| Na | < 300 |
| Si | 3.5 |

Analytical Technique: inductively coupled plasma