Certificate of Analysis

Graphite (C)

APS: 100 nm, Purity: 99%

Stock #:  1249YD

| Components | Contents (ppm) |
| --- | --- |
| B | < 50 |
| Ca | < 300 |
| Cu | < 20 |
| Fe | < 30 |
| Mn | < 20 |
| Pb | < 5 |
| Si | < 300 |