Certificate of Analysis

Cobalt (Co)

99.8% (metal basis)

APS 28 nm

Stock #: 0276JY

| Components | Contents (%) |
| --- | --- |
| Cr | 0.0002 |
| Fe | 0.01 |
| Mn | 0.003 |
| Ni | 0.08 |
| Si | 0.004 |

Analytical technique: inductively coupled plasma emission spectroscopy