Certificate of Analysis

Cobalt-Zinc Iron Oxide (Co0.5Zn0.5Fe2O4)

# Purity: 98.5%,  APS: 15-30 nm

Stock #:  1515FY

| Components | Contents (%) |
| --- | --- |
| Al | 0.07 |
| Ca | 0.25 |
| Mg | 0.38 |
| Mn | 0.18 |
| Na | 0.18 |

Analytical Technique:  inductively coupled plasma

Nanostructured & Amorphous Materials, Inc.

17702 Emerald Garden Lane, Houston, TX 77084, USA 
Phone: (281) 858-6571 ( Fax: (281) 858-6507

E-mail: sales@nanoamor.com ( Website: http://www.nanoamor.com