Certificate of Analysis

Copper (Cu)

99.99% (metal basis)

APS 40 nm

Stock #: 0296JY

| Components | Contents (%) |
| --- | --- |
| Ag | 0.001 |
| Ca | 0.001 |
| Mn | 0.0001 |
| Si | 0.10 |

Analytical technique: inductively coupled plasma emission spectroscopy