Certificate of Analysis

Copper Oxide (CuO)

APS 40 nm, 99.9%

Stock #:  2110FY

| Components | Contents (ppm) |
| --- | --- |
| Ba | 0.8 |
| Ca | 400 |
| Cd | 2.4 |
| Co | 6.4 |
| Fe | 87 |
| K | 300 |
| Mg | 72 |
| Mn | 3.2 |
| P | 300 |
| Pb | 100 |
| Sr | 2.4 |
| Zn | 200 |

Analytical Technique: inductively coupled plasma