Certificate of Analysis

Iron (Fe)

99.95% (metal basis)

APS 25 nm

Stock #: 0266JY

| Components | Contents (%) |
| --- | --- |
| Ca | 0.004 |
| Cr | 0.006 |
| Mn | 0.012 |
| Ni | 0.008 |
| Si | 0.02 |

Analytical technique: inductively coupled plasma emission spectroscopy