Certificate of Analysis

Gadolinium oxide, 20 - 80 nm, 99.9+%(REO)

Stock #: 2680ZQ

| Components | Contents (%) |
| --- | --- |
| REO | Dy2O3 | < 0.01 |
|  | Eu2O3 | 0.031 |
|  | Sm2O3 | < 0.01 |
|  | Tb4O7 | < 0.01 |
|  | Y2O3 | < 0.01 |
| Non-REO | CaO | 0.008 |
|  | Fe2O3 | 0.004 |
|  | SiO2 | 0.006 |

Analytical Technique: inductively coupled plasma