Certificate of Analysis

Indium oxide, 20 - 100 nm, 99.99%

Stock #: 2710TN

| Components | Contents (ppm) |
| --- | --- |
| Cr | < 5 |
| Sb | < 5 |
| Cd | < 5 |
| Cu | < 5 |
| Fe | < 8 |
| Pd | < 15 |
| Ni | < 5 |
| Si | < 10 |
| Zn | < 5 |
| Sn | < 15 |

Analytical Technique:

Inductively coupled plasma – atomic emission spectroscopy (ICP-AES)