Certificate of Analysis

Nickel Iron Oxide (NiFe2O4)

APS 30 nm, 99.9%

| Components | Contents (ppm) |
| --- | --- |
| Ba | 3.4 |
| Ca | 2100 |
| Co | 92 |
| Cr | 15 |
| Cu | 24 |
| Mg | 300 |
| Mn | 830 |
| Na | 3100 |
| Sr | 14 |
| Zn | 48 |

Analytical Technique: inductively coupled plasma