Certificate of Analysis

Nickel-Zinc Iron Oxide (Ni0.5Zn0.5Fe2O4)

# Purity: 99.9%, APS: 40 nm

| Components | Contents (%) |
| --- | --- |
| Ca | 0.31 |
| Co | 0.013 |
| Mg | 0.67 |
| Mn | 0.17 |
| Na | 0.09 |
| Si | 0.004 |

Analytical Technique:  inductively coupled plasma

Nanostructured & Amorphous Materials, Inc.

17702 Emerald Garden Lane, Houston, TX 77084, USA 
Phone: (281) 858-6571 ( Fax: (281) 858-6507

E-mail: sales@nanoamor.com ( Website: http://www.nanoamor.com