Certificate of Analysis

Praseodymium oxide
APS: 50 nm

Purity: 99.9% (REO)

| Components | Contents (%) |
| --- | --- |
| REO | CeO2 | < 0.05 |
|  | La2O3 | < 0.01 |
|  | Nd2O3 | < 0.40 |
|  | Sm2O3 | < 0.01 |
|  | Y2O3 | < 0.01 |
| Non-REO | CaO | < 0.0047 |
|  | CuO | < 0.0001 |
|  | Fe2O3 | < 0.0016 |
|  | SiO2 | < 0.01 |

Analytical Technique:  Inductively coupled plasma  (ICP)

Nanostructured & Amorphous Materials, Inc.

17702 Emerald Garden Lane, Houston, TX 77084, USA 
Phone: (281) 858-6571 ( Fax: (281) 858-6507

E-mail: sales@nanoamor.com ( Website: http://www.nanoamor.com