Certificate of Analysis

Titanium oxide (anatase)

APS: 10 nm, Purity: ≥ 99.99%

Stock #: 5425HT

| Components | Contents (ppm) |
| --- | --- |
| Al | ≤ 20 |
| Ca | ≤ 75 |
| Mg | ≤ 65 |
| Nb | ≤ 119 |
| S | ≤ 165 |
| Si | ≤ 102 |