Certificate of Analysis

Tungsten (W)

99.5%, APS 65 nm

Stock #: 0743WF

| Components | Contents (%) |
| --- | --- |
| Al | 0.082 |
| Cr | 0.0068 |
| Fe | 0.0223 |
| K | 0.0066 |
| O | 0.2245 |

Analytical Technique: x-ray fluorescence spectrometer