Certificate of Analysis

Silver (Ag)

APS 30-50 nm, 99.9+%

Stock #:  0477YD

| Components | Contents (ppm) |
| --- | --- |
| Al | 10 |
| As | < 0.5 |
| Bi | 20 |
| Cu | 17 |
| Fe | 56 |
| Ni | 3 |
| Pb | 9 |
| Sb | < 0.5 |
| Si | 41 |

Analytical Technique:  inductively coupled plasma