Sapphire ( single crystal of Al2O3 ) is being used extensively as a substrate for III-V nitrides and for many other epitaxial films.  MTI has been supplying sapphire substrates since 1991 for research and industry. In order to meet the increasing demand for blue LED and LD devices,  MTI has built up a venture in China  to mass produce high quality sapphire crystal and epi polished wafer at the most competitive price.  Our excellent specialists, advanced growth technology and state of art polishing facilities allow us to become one of the largest suppliers for sapphire crystal and wafer in the world.

|  | Physical Properties of Sapphire |
| --- | --- |
| Crystal Structure | Hexagonal. a =4.758 Å c= 12.992 Å |
| Crystallographic D spacing | (1120 ) - a plane: 2.379 Å (1102) - r plane: 1.740 Å (1010) - m plane: 1.375 Å (1123) - n plane: 1.147 Å¯ (0001) - c plane: 2.165 Å (1011) - s plane: 1.961 Å |
| Crystal Purity | > 99.99% |
| Melt Point | 2040 oC |
| Density | 3.98 g/cm3 |
| Hardness | 9 ( mohs) |
| Thermal Expansion | 7.5 (x10-6/ oC) |
| Specific Heat | 0.10 ( cal / oC) |
| Thermal Conductivity, | 46.06 @ 0 oC 25.12 @ 100 oC, 12.56 @ 400 oC ( W/(m.K) ) |
| Dielectric Constant | ~ 9.4 @300K at A axis ~ 11.58@ 300K at C axis |
| Loss Tangent at 10 GHz | < 2x10-5 at A axis , <5 x10-5 at C axis |
| Standard Products |
| As - grown boules <0001> ori.± 0.5o | 3" dia x 50 ~ 70 mm length 2" dia x 50 ~ 70 mm length 30 mm dia x 150 mm length |
| As-cut blanks <0001> ori.± 0.5o | 2" dia x 0.7 mm thickness 1" dia x 0.7 mm thickness |
| Epi -polished substrates C, R, A plane: ori.± 0.5o 1 or 2 sides polished Ra< 10 Å | 3" dia. x 0.5 mm 2" dia. x 0.33 mm, 2"dia x 0.5 mm 1" dia x 0.5 mm 0.5" x 0.5" x 0.5 mm 10x10x0.5 mm |

Special size and orientation are available upon request

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4058   E-mail: info@mtixtl.com   Website: www.mtixtl.com

# Text boxes

Al2O3 Single Crystal

Sapphire boule and polished wafer