Crystal Properties

| Parameter | Unit | Figure |
| --- | --- | --- |
| Crystal Class |  | Cubic |
| Point Group |  | 23 |
| Space Group |  | I213 |
| Lattice Parameter | nm | a 1.10146 |
| Melting Point | ℃ | 930 |
| Density | g/cm3 | 9.2 |
| Hardness | Mohs | 4.5 |
| dielectric Constant |  | εS11/ε0 39.4、εT33/ε0 43.4 |
| Elastic Stiffness Coefficient | x1011N/m2 | CE11 1.29、CE44 0.26 |
| Piezoelectric Strain Constant | C/m2 | e14 0.89 |
| Transparency Range | nm | 470~7500 |
| Electro-optic Coefficient | x10-12m/V | r41 3.4 |
| Refractive Index |  | 2.55 |
| Gradient of Refractive index | x10-5/cm | ≤5 |
| Optic Activity | mm-1 | Left20°@ 632.8nm |
| Transitivity | % | 67 @ 632.8nm |

Typical SAW Properties

| Cute Type | Vs (m/s) | K2s (%) | TCV(10-6/ oC) | TCD(10-6/oC) |
| --- | --- | --- | --- | --- |
| [110]-[001] | 1624 | 0.70 | -105 | 128 |
| [001]-[110] | 1680 | 1.30 | -117 | 140 |

| Applications Surface Acoustic Wave (SAW) Device. Bulk Acoustic Wave (BAW) Device. Holographic Memory. Eiectro-optic device. |  |
| --- | --- |

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4058   E-mail: info@mtixtl.com   Website: www.mtixtl.com

# Text boxes

Bi12GeO20

New Generation acousto-optic crystal