BeO Ceramic Properties

Property Condition Unit Value Density g/cm 3 ≥2.85 BeO purity % ≥99 Tensile strength MPa ≥140 linear expansion coeff. 20℃-500℃ ×10 -4 /℃ 7-8.5 Thermal Conductivity 40℃ W/m·k ≥250 Specific Heat 25℃ cal/°C gm 0.25 Hardness 60 Rockwell Dialectic Constant 1MHz 20℃ 6.5-7.5 10GHz 20℃ 6.5-7.5 1MHz 20℃ ×10 -4 ≤4 10GHz 20℃ ×10 -4 ≤8 Resistivity 100℃ Ω.cm ≥1013 300℃ Ω.cm ≥1010 Dialectic Strength DC KV/mm ≥15 Chemical stability 1:9HCl ug/cm 2 ≤0.3 10% NaOH ug/cm 2 ≤0.2 Max. working Temperature ℃ 1800