Calcite is a negative uniaxial crystal that has high birefringence, wide spectral transmission and availability in reasonably sized rhombs. It’s good material used as visible and near IR polarizers.   MTI carefully inspects the raw calcite crystals which is grown by nature, and provides Calcite component with the highest quality and lowest price

|  | Typical Properties |
| --- | --- |
| Crystal structure | Rhomb. a= 4.989 c= 17.062 |
| Melting point | 1339 oC |
| Density | 2.71 g/cm3 |
| Transparency Range | 350nm - 2300nm |
| Hardness | 3 Mohs |
| Thermal expansion Coefficient | (a = 24.39 ( 10-6/K; (c = 5.68 ( 10-6/K |
| Crystal Class | Negative uniaxial with (o=(a=(b , (e=(c |
| Refractive Index | (o = 1.6557, (e = 1.4852, (( = -0.1705, ( = 6.20o at 0.63 (m (o = 1.6629, (e = 1.4885, (( = -0.1744, ( = 6.32o at 1.30 (m |
| Hygroscopic Susceptibility | Low susceptibility to moisture |
| Sellmeier Equation ( ( in (m ) |
| (o2 = 2.69705 + 0.0192064/((2 –0.01820) – 0.0151624 ( (2 (e2 = 2.18438 + 0.0087309/((2 –0.01018) – 0.0024411 ( (2 |
| Specifications |
| Crystal Dimension | Crystal bulk: up to 50 x 50 x 30 mm as cleaved Crystal wafer: 10x10x0.5 mm 2 sides polished 1”x1”x1.0 mm 2”x2”x1.2 mm |
| Surface Quality | 20/10 Scratch and Dig |
| Dimension tolerance | ( 0.1 mm |
| Beam Deviation | < 3 arc min. |
| Optical axis orientation | +/- 0.5o |
| Flatness | (/4 @ 632.8 nm |
| Transmission wavefront distortion | < (/2 @ 632.8 nm |
| AR-coating | Reflectance < 0.5% |

------------------------------------------------------------------------------------------------------------------------------------------

### MTI Corporation

2700 Rydin Road, Unit D, Richmond, CA 94804, USA

Tel:(510) 525-3070     Fax:(510) 525-4705   E-mail: info@mticrystal.com  Website: www.mticrystal.com

# Text boxes

#### Calcite Crystal

(CaCO3)