CdTe and CdZnTe (CTZ) Crystal

CdTe and CZT crystal are new semiconductor which enables to convert radiation to electron effectively, It will reform radiography and radiation measurement in medical and industrial area. MTI  provides both of CdTe and CZT crystal for researcher and industrial at the best quality at competitive price.

|  | CdTe | CdZnTe |
| --- | --- | --- |
| Growth Method Low R: 5x104 | Bridgman | Bridgman |
| Structure | Cubic F43m | Cubic F43m |
| Lattice Constant (Å) | a = 6.483 | a = 6.483 – 6.446 |
| Mol. weight | 240.01 | 81.39 |
| Density ( g/cm3) | 5.851 | 5.605 |
| Melting Point (oC) | 1047 | 1975 |
| Heat Capacity (J /g.k) | 0.210 | 0.125 cal/gm |
| Thermal Expansion (10-6 /K) | 5.0 | 6.5 // a 3.7 // c |
| Thermal Conductivity ( W /m.k at 300K ) | 6.3 | 30 |
| Transparent wavelength (µ) | 0.85 ~ 29.9 | 0.4 ~ 0.6 |
| Refractive Index | 2.72 | 1.922 (o) 1.936 (e) |
| Conductivity | P type ( N type available for hi R only upon request ) | P type ( N type available upon request ) |
| Resistivity (ohm-cm) | Low R: ~ 8x104 High: R: ~ 106 ~108 | Low R: 5x104 High: R:> 106 |
| Carrier concentration ( cm-3 ) | Low R: ~ 9x1014 High: R: < 1010 | Low R: ~ 1015 High: R: ~ 1012 |
| Max. Crystal size (mm ) | 20 x 20 x 10 | 20x20x10 |

MTI Corporation                                                                         www.mtixtl.com

860 South 19th Street,  CA 94804, Richmond,  CA 94804, USA

Tel: (510)525-3070     Fax: (510)525-4705         E-mail:  info@mtixtl.com