New Scintillation Crystal  Ce:Lu2SiO5

Ce doped Lu2SiO5 crystal is a new scintillation crystal, which is using for x-ray inspection, medical examination and space physics.  MTI supplies high quality Ce: Lu2SiO5 crystal boule up to 2” diameter.

Typical Properties

| Crystal Structure Point Group Space Group | Trigonal 2/m C2/c |
| --- | --- |
| Lattice Constant ( A) | a =14.254、b =10.241、c =6.641、γ =122.20 Deg |
| Melting Point | 2047 ℃ |
| Density | 37.3～7.4 g/cm |
| Hardness | 5.8 Moh |
| Refractive Index | 1.82 |
| Emission wavelength | 418 nm |
| Relative emission Intensity | 75% relative to NaI |
| After glow | 40 ns |
| Resistant to radiation | ＞1×108 Rad |
| Moisture | No |
| Typical Crystal axis | Z cut |
| Typical crystal Boule Dimension | Max. Diameter : 2” Max Length: 2.5” |
| Crystal growth Technology | CZ |

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4058   E-mail: info@mtixtl.com   Website: www.mtixtl.com