UV Optical Grade Fused Silica

Optical UV grade Fused Silica is a high purity synthetic amorphous silicon dioxide which is manufactured by flame hydrolysis. Some beneficial characteristics indlude very low thermal expansion coefficient, very good homogeneity with excellent optical properties and exceptional transmittance in the UV range. It has been used widely for Laser optics, optical grade UV Fused Silica windows and lenses, mirror blanks and substrates, wedges, optical beamsplitters and filters, prisms, lightpipes, space and aircraft windows, solar cells, high quality coating substrates etc.  MTI supplies UV grade fused silica up to 8” diameter with thickness from 0.1 mm  to 6.3 mm

Typical Properties of UV Grade Fused Silica

| Coefficient of Thermal Expansion (CTE): | 0.52 ppm/K @ 5-35ºC 0.57 ppm/K @ 0-200ºC 0.48 ppm/K @ -100 - 200ºC | Strain Point | 893°C/1639.4°F |
| --- | --- | --- | --- |
| Young's Modulus | 72.1 GPa | Annealing Point | 1042°C/1907.6°F |
| Shear Modulus | 30.6 GPa | Softening Point | 1585°C/2885°F |
| Modulus of Rupture, abraded: 52.4 MPa | 52.4 MPa | Annealing Point | 1042°C/1907.6°F |
| Bulk Modulus | 37.4 GPa | Thermal Conductivity | 1.38 W/mK |
| Poisson's Ratio | 0.179 | Thermal Diffusivity: . | .0075 cm2/s |
| Density (at 25ºC / 77ºF) | 2.201 g/cm3 |  |  |
| Knoop Hardness | 522 kg/mm2 (100g load) | Dielectric Constant: | E= 3.8 |
| Compressive Strength: | 1.14 GPa | Refractive Index: | nD = 1,45840 (589nm) |
| Tensile Strength | 54 MPa | Optical transmission | See picture below |

MTI Corporation

2700 D Rydin Road, Richmond, CA 94804 USA

tel: 510-525-3070  Fax: 510-525-4705  Email: info@mtixtl.com Website: www.mtixtl.com