|  | Physical Properties of Sapphire |
| --- | --- |
| Crystal Structure | Cubic: a =12.376 Å , ( Z = 8 ) |
| Molecular weight | 1012.365 |
| Melt Point | 1800 oC |
| Density | 7.09 g/cm3 |
| Hardness | ~ 8 ( mohns) |
| Refractive index | 1.95 |
| Crystal Purity | > 99.99% |
| Crystal growth method | Czochralski |
| Crystal growth direction | <111> |
| Standard Specs of GGG crystal substrates |
| Max. Crystal boule | 3” dia x 100 mm length |
| Standard substrate size At Orientation <111> ±0.5 o | 3” dia. X 0.5 mm , two sides epi polished 10 x 10 x 0.5 mm, two sides epi polished |

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4058   E-mail: info@mtixtl.com   Website: www.mtixtl.com

# Text boxes

GGG

Gd3Ga5O12 single crystal and substrate