Material

Structure

Mercury Cadmium Telluride

Specification Summary

Generic Name       Mercury Cadmium Telluride

Also known as       MCT, CMT, MerCadTel

Formula       Hg1-XCdXTe

Stock X Range       Mean X from 0.160 to 0.420 (other values on request)

Growth Technique       Bulk, Modified Bridgeman

Extrinsic Dopants       None

Conductivity Type       n-type (p-type on request)

Orientation       Undefined

Crystallography       One grain (typical), two grains (max)

Surface Finish       Mechanical-chemical mirror polish (both sides)

Flatness       ± 20 µm across wafer surface (excluding outer edge which is radiused)

Smoothness       ± 2 µm

Parallelism       to 20 µm, typically convex

Defects      To the naked eye minimal precipitates/pits, no holes, no cracks

| Geometry Thickness 500 ± 100 µm |
| --- |
| Shape Planar Dimensions Area Orientation Index (optional) | Wafer (circular) Diameter 15.5 ± 0.6 mm (nominal) 180 sq mm (nominal) Flat and/or groove | Plank (rectangular) 15 x 20 mm (max), 9.5 x 9.5 mm (min) from 300 down to 90 sq mm Bevelled corner |

| Characteristics at various X values Mean X |
| --- |
| Cut-on wavelength, 77K (µm) Cut-on wavelength, 300K (µm) | 0.180 24.6 9.8 | 0.210 12.5 7.4 | 0.270 6.4 5.0 | 0.350 3.9 3.5 |
| Conductivity Type n-type |
| Carrier Concentration (CC) @77K Mobility (Mu) @77K | 1E14 < CC < 1E15 Mu >= 1E5 | 5E13 < CC < 5E14 Mu >= 5E4 | 2E13 < CC < 5E14 Mu >= 2E4 | 5E12 < CC < 1E13 Mu >= 5E3 |
| CC units are cm-3 Mu units are cm2/V.s |

| X Uniformity Grades |
| --- |
| Across wafer/plank Between centre four scan points | A-grade Mean X ± 0.005 Mean X ± 0.003 | B-grade Mean X ± 0.010 Mean X ± 0.005 |