KTN Single Crystal ---- New Generation Electric-Optical Crystal

Single crystal  KTN   ( KTa 1-X NbXO3 )  is transparent isotropic crystal with very large electro-optic coefficients of about >600 pm/V, which is 20 times larger than that of conventional LiNbO3.  Also, it is excellent substrate for ferroelectric thin film

KNT crystal is grown by top seeded flux method, which requires precision temperature control and extreme slow pulling rate. Now it is very expensive. However, MTI believes we can make cost down with increasing market demand

Typical Properties

| Chemistry | ( KTa 1-X NbXO3 ) |
| --- | --- |
| Crystal growth method: | Top seed flux growth |
| Crystal Structure: | Cubic, Perovskite, a = 3.989 -4.0A depended on Nb doped |
| Melting point: | Does not melt congruently. |
| Curie Temperature | 20- 30 oC |
| Density: | 7.015 g / cc |
| Thermal conductivity: | 0.17 w/m.k at 300k |
| Linear Eelectric - Optical Coeff | r33 : > 600 pm/V |
| Refractive index: | 2.234 |
| Coercive Field | Ec = 250 V/mm |
| Transmission Range | 400 nm - 4000 nm |
| Standard substrates size | 10x10x0.5 mm, <100> 5 x 5 x 0.5 mm. <100> |

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4058   E-mail: info@mtixtl.com   Website: www.mtixtl.com