LaAlO3 single crystal provides a good lattice match to many materials with perovskite structure. It is an excellent substrate for epitaxial growth of high Tc superconductors , magnetic and ferro-electric thin films. The dielectric properties of LaAlO3  crystal are well suitable for low loss microwave and dielectric resonance applications.

MTI is the largest existing grower of LaAlO3 single crystals. It produces 10- 20 Kg of LaAlO3 crystals per month and can supply as-grown boules, as-cut blanks and epi-polished substrates up to 3” diameter.  The surface roughness of MTI  LaAlO3 substrate is warranted  less than 8 Å through in house AFM quality control.

|  | Typical Physical Properties |
| --- | --- |
| Crystal Structure | Rhombohedral at 25 oC: a=3.79 Å c= 13.11 Å Cubic at > 435 oC : a=3.821 Å |
| Growth Method | Czochralski |
| Density | 6.52 g/cm3 |
| Melt Point | 2080 oC |
| Thermal expansion | 10 (x10-6/ oC) |
| Dielectric Constant | ~ 25 |
| Loss Tangent at 10 GHz | ~3x10-4 @ 300K , ~0.6 x10-4 @77K |
| Color and Appearance | Tan to Brown based on annealing condition Visible twins on polished substrate. |
| Chemical Stability | Insoluble in mineral acids at 25 oC and soluble in H3PO3 at> 150 oC |
| Standard Products |
| As - grown boule <100> | 3" dia x 50 ~ 70 mm length 2" dia x 50 ~ 70 mm length |
| As cut blank <100> | 3” dia x 0.7 mm , 2" dia x 0.7 mm 1" dia x 0.7 mm |
| Epi -polished substrates <100> ori. 1 or 2 sides polished Ra< 8 Å by AFM certified | 3”dia x 0.5 mm, 2" dia x 0.5 mm 1" dia x 0.5 mm 1”x1”x0.5 mm 0.5" x 0.5" x 0.5 mm 10x10x0.5 mm |

# Special size and orientation are available upon request

_____________________________________________________________________________________

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4058   E-mail: info@mtixtl.com   Website: www.mtixtl.com

# Text boxes

3”  and 2” dia. LAO boules

3” dia. LAO blank and polished wafer

LaAlO3 Single Crystal