MgAl2O4 ( spinel ) single crystals are widely used for bulk acoustic wave and microwave devices and fast IC epitaxial substrates. It is also found that MgAl2O4 is a good substrate for III-V nitrides device.  MgAl2O4 crystal is very difficult to grow, due to the difficulty in maintaining a single phase structure.  Following several year of effort, MTI is proud of being able to supply the best quality MgAl2O4 crystal in the world.

|  | Typical Physical Properties |
| --- | --- |
| Crystal Structure | Cubic: a = 8.083 Å |
| Growth Method | Czochralski |
| Density | 3.64 g/cm3 |
| Melt Point | 2130 oC |
| Hardness | 8.0 ( Mohns) |
| Thermal expansion | 7.45 (x10-6/ oC) |
| Phase Velocity | 6500 m/s at (100> shear wave |
| Propagation loss | 6.5 dB/(s |
| Typical growth direction | <100> and <110> |
| Standard Products |
| As-grown boule <100> ori. ± 0.5o | 35 mm dia x 60 mm length |
| As-cut blank <100>, <111> , <110>± 0.5o | 32 mm dia x 0.7 mm with <011>OF |
| Epi -polished substrates <100>, <111> , <110>± 0.5o 1 or 2 sides polished Ra< 8 Å | 32 mm dia x 0.5 mm 1" dia x 0.5 mm 10x10x0.5 mm |

Special size and orientation are  available upon request

________________________________________________________________________________

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4058   E-mail: info@mtixtl.com   Website: www.mtixtl.com

# Text boxes

MgAl2O4 Crystal

(Spinel )