SrLaGaO4 Single Crystal

Single crystals of SrLaAlO4 (SLAO) are the attractive compounds used as substrates for high

temperature superconductor thin films.  High quality YBaCu, BiSrCaCuO, Bi(Pb)CaCuO and

TlBaCaCuO thin films have been grown on SrLaAlO4 substrates by different techniques.

TECHNICAL DATA

| Crystal growth method | Czochralski |
| --- | --- |
| Crystal growth orientation | <100> ; <110> ; <001> |
| Maximum wafer diameter | < 1 inch |
| Standard sizes | 10 mm x 10 mm |
| Standard thickness | 0,5 ÷ 1 mm |
| Surface quality | one- or both side epipolished |
| CRYSTALLOGRAPHIC PROPERTIES |
| Space group | I4/mmm |
| Crystallographic structure | tetragonal |
| Lattice constant | a = 0,3843 nm c = 1,2680 nm |
| Twinning structure | No |
| Colour | Colorless-Yellow |
| PHYSICAL PROPERTIES |
| Density | 6,389 g/cm3 |
| Melting point | 1520°C |
| Hardness | at <001> : 7394 MPa at <100> : 7119 MPa |
| Thermal expansion coefficient | along a-axis : 10,05 x 10-6 K-1 along c-axis : 18,90 x 10-5 K-1 |
| Dielectric constant | 22 |
| Dielectric loss tangent | 5,7 x 10-5 |
| Electrical character | dielectric |

MTI Corporation

860 South 19th Street, Richmond,  CA 94804, USA

Tel: (510)525-3070  Fax: (510)525-4058   E-mail: info@mtixtl.com   Website: www.mtixtl.com