Certificate of Analysis

Typical Properties

| Sample | Color | Purity (%) | Structure | Average Particle Size (nm) | Morphology |
| --- | --- | --- | --- | --- | --- |
| Si | brown yellow | 99.42 | crystalline | 100 | spherical |

Chemical analysis:  Quantitative Result

| Element | Analysis Results by Wet Chemical, Wt % |
| --- | --- |
| Si | > 99.0 |
| Al | < 0.02 |
| Ca | <0.001 |
| C | < 0.020 |
| Cu | < 0.0042 |
| Cr | < 0.001 |
| Fe | <0.015 |
| Ni | <0.0085 |
| O | Rest ( Typical <0.50 ) |

TEM & XRD Analysis

| TEM photo: Shows average particle size of Si < 100 nm | XRD Curve: shows Nano Si powder is crystalline structure |
| --- | --- |

# Text boxes

MTI Corporation

860 South 19th Street, CA 94804, USA

tel: 510-525-3070   fax 510-525-4705 email: info@mtixtl.com  web: www.mtixtl.com