Certificate of Analysis

Silicon Carbide, Beta

Size: 40nm,  Purity: 99%

Item Number: NP-SiC-40

| Components | Contents (%) |
| --- | --- |
| Si | 69.37 |
| C | 29.63 |
| O | 0.09 |
| N | 0.07 |

Analytical Techniques:

Gas-volumetric method

IR detector

Potential measurement