DX-100 machine and Bragg Law

Bragg's Law       n = 2d sinHere  = 0.154056 nm for Cu (Kα) X-ray

For more information on Bragg's Law and Diffraction, please see the link

http://www.eserc.stonybrook.edu/ProjectJava/Bragg/

When measure a single crystal sample orientation:

- Calibrate DX-100 by standard sample.

- Find the theoretical Ө angle of oriented single crystal sample. (From ICDD data base)

- Set the detector at 2Ө angle position.

- Set the sample at Ө angle position.

- Rotate Ө angle (sample) to find Max. diffraction intensity (mV meter)

- The Ө angle displayed in Max. Diffraction intensity is real angle of sample orientation. If the value is deviated from theoretical value, it means the crystal sample is out of orientation.

# Text boxes

Sample to measure

Detector setting for 2Ө

X-Ray Tube

Ө angle

2Ө angle